Standards：

IEC60092-350

IEC60092-351

IEC60092-352

IEC60092-353

IEC60092-359

IEC60228

IEC60332

Application：

The cable is intended for power, lighting and control system of marine and off-shore building, and it is also available to metallurgical industry, chemical works, power plant and mine etc.

1-      conductor Tinned copper wire

2-      Insulation EPR, PVC

3-      Filler

4-      Tape

5-      Inner sheath PCP, CSP, PVC

6-      Armour Tinned copper wire or galvanized

7-      Outer sheath PVC

| 型号 Type | 名称 Description | 产品标准 Standard |
| --- | --- | --- |
| CEF/DA | 乙丙绝缘氯丁护套船用电力电缆，DA型 EPR insulation PCP sheath shipboard power cable, Type DA | IEC60092-350 IEC60092-353 IEC60332-1 IEC60332-3A |
| CEF80/DA | 乙丙绝缘氯丁内护套镀锡铜丝编织铠装船用电力电缆，DA型 EPR insulation PCP inner sheath tinned copper wire braided shipboard power cable, Type DA |  |
| CEF90/DA | 乙丙绝缘氯丁内护套镀锌钢丝编织铠装船用电力电缆，DA型 EPR insulation PCP inner sheath galvanized steel wire braided shipboard power cable, Type DA |  |
| CEF82/DA | 乙丙绝缘氯丁内护套镀锡铜丝编织铠装聚氯乙烯外护套船用电力电缆，DA型 EPR insulation PCP inner sheath tinned copper wire braided PVC outer sheathed shipboard power cable, Type DA |  |
| CEF92/DA | 乙丙绝缘氯丁内护套镀锌钢丝编织铠装聚氯乙烯外护套船用电力电缆，DA型 EPR insulation PCP inner sheath galvanized steel wire braided PVC outer sheathed shipboard power cable, Type DA |  |
| CEF/SA | 乙丙绝缘氯丁护套船用电力电缆，SA型 EPR insulation PCP inner sheath shipboard power cable, Type SA |  |
| CEF80/SA | 乙丙绝缘氯丁内护套镀锡铜丝编织铠装船用电力电缆，SA型 EPR insulation PCP inner sheath tinned copper wire braided shipboard power cable, Type SA |  |
| CEF90/SA | 乙丙绝缘氯丁内护套镀锌钢丝编织铠装船用电力电缆，SA型 EPR insulation PCP inner sheath galvanized steel wire braided shipboard power cable, Type SA |  |
| CEF82/SA | 乙丙绝缘氯丁内护套镀锡铜丝编织铠装聚氯乙烯外护套船用电力电缆，SA型 EPR insulation PCP inner sheath tinned copper wire braided PVC outer sheathed shipboard power cable, Type SA |  |
| CEF92/SA | 乙丙绝缘氯丁内护套镀锌钢丝编织铠装聚氯乙烯外护套船用电力电缆，SA型 EPR insulation PCP inner sheath galvanized steel wire braided PVC outer sheath shipboard power cable, Type SA |  |

| 型号 Type | 名称 Description | 产品标准 Standard |
| --- | --- | --- |
| CEH/DA | 乙丙绝缘氯磺化聚乙烯护套船用电力电缆，DA型 EPR insulation CSP sheath shipboard power cable, Type DA | IEC60092-350 IEC60092-353 IEC60332-1 IEC60332-3A |
| CEH80/DA | 乙丙绝缘氯磺化聚乙烯内护套镀锡铜丝编织铠装船用电力电缆，DA型 EPR insulation CSP inner sheath tinned copper wire braided shipboard power cable, Type DA |  |
| CEH90/DA | 乙丙绝缘氯磺化聚乙烯内护套镀锌钢丝编织铠装船用电力电缆，DA型 EPR insulation CSP inner sheath galvanized steel wire braided shipboard power cable, Type DA |  |
| CEH82/DA | 乙丙绝缘氯磺化聚乙烯内护套镀锡铜丝编织铠装聚氯乙烯外套船用电力电缆，DA型 EPR insulation CSP inner sheath tinned copper wire braided PVC outer sheath shipboard power cable, Type DA |  |
| CEH92/DA | 乙丙绝缘氯磺化聚乙烯内护套镀锌钢丝编织铠装聚氯乙烯外套船用电力电缆，DA型 EPR insulation CSP inner sheath galvanized steel wire braided PVC outer sheath shipboard power cable, Type DA |  |
| CEH/SA | 乙丙绝缘氯磺化聚乙烯护套船用电力电缆，SA型 EPR insulation CSP sheath shipboard power cable, Type SA |  |
| CEH80/SA | 乙丙绝缘氯磺化聚乙烯内护套镀锡铜丝编织铠装船用电力电缆，SA型 EPR insulation CSP inner sheath tinned copper wire braided shipboard power cable, Type SA |  |
| CEH90/SA | 乙丙绝缘氯磺化聚乙烯内护套镀锌钢丝编织铠装船用电力电缆，SA型 EPR insulation CSP inner sheath galvanized steel wire braided shipboard power cable, Type SA |  |
| CEH82/SA | 乙丙绝缘氯磺化聚乙烯内护套镀锡铜丝编织铠装聚氯乙烯外套船用电力电缆，SA型 EPR insulation CSP inner sheath tinned copper wire braided PVC outer sheath shipboard power cable, Type SA |  |
| CEH92/SA | 乙丙绝缘氯磺化聚乙烯内护套镀锌钢丝编织铠装聚氯乙烯外套船用电力电缆，SA型 EPR insulation CSP inner sheath galvanized steel wire braided PVC outer sheath shipboard power cable, Type SA |  |

| 型号 Type | 名称 Description | 产品标准 Standard |
| --- | --- | --- |
| CEV/DA | 乙丙绝缘聚氯乙烯护套船用电力电缆，DA型 EPR insulation PVC sheath shipboard power cable, Type DA | IEC60092-350 IEC60092-353 ICE60332-1 IEC60332-3A |
| CEV80/DA | 乙丙绝缘聚氯乙烯内护套镀锡铜丝编织铠装船用电力电缆，DA型 EPR insulation PVC inner sheath tinned copper wire braided shipboard power cable, Type DA |  |
| CEV90/DA | 乙丙绝缘聚氯乙烯内护套镀锌钢丝编织铠装船用电力电缆，DA型 EPR insulation PVC inner sheath galvanized steel wire braided shipboard power cable, Type DA |  |
| CEV82/DA | 乙丙绝缘聚氯乙烯内护套镀锡铜丝编织铠装聚氯乙烯外护套船用电力电缆，DA型 EPR insulation PVC inner sheath tinned copper wire braided PVC outer sheath shipboard power cable, Type DA |  |
| CEV92/DA | 乙丙绝缘聚氯乙烯内护套镀锌钢丝编织铠装聚氯乙烯外护套船用电力电缆，DA型 EPR insulation PVC inner sheath galvanized steel wire braided PVC outer sheath shipboard power cable, Type DA |  |
| CEV/SA | 乙丙绝缘聚氯乙烯护套船用电力电缆，SA型 EPR insulation PVC sheath shipboard power cable, Type SA |  |
| CEV80/SA | 乙丙绝缘聚氯乙烯内护套镀锡铜丝编织铠装船用电力电缆，SA型 EPR insulation PVC inner sheath tinned copper wire braided shipboard power cable, Type SA |  |
| CEV90/SA | 乙丙绝缘聚氯乙烯内护套镀锌钢丝编织铠装船用电力电缆，SA型 EPR insulation PVC inner sheath galvanized steel wire braided shipboard power cable, Type SA |  |
| CEV82/SA | 乙丙绝缘聚氯乙烯内护套镀锡铜丝编织铠装聚氯乙烯外护套船用电力电缆，SA型 EPR insulation PVC inner sheath tinned copper wire braided PVC outer sheath shipboard power cable, Type SA |  |
| CEV92/SA | 乙丙绝缘聚氯乙烯内护套镀锌钢丝编织铠装聚氯乙烯外护套船用电力电缆，SA型 EPR insulation PVC inner sheath galvanized steel wire braided PVC outer sheath shipboard power cable, Type SA |  |

| 型号 Type | 名称 Description | 产品标准 Standard |
| --- | --- | --- |
| CE8F/DA | 乙丙绝缘镀锡铜丝编织铠装氯丁外护套船用电力电缆，DA型 EPR insulation tinned copper wire braided PCP outer sheath shipboard power cable, Type DA | IEC60092-350 IEC60092-353 IEC600332-1 |
| CEF8F/DA | 乙丙绝缘氯丁内护套镀锡铜丝编织铠装氯丁外护套船用电力电缆，DA型 EPR insulation PCP inner sheath tinned copper wire braided PCP outer sheathed shipboard power cable, Type DA |  |
| CE8H/DA | 乙丙绝缘镀锡铜丝编织铠装氯磺化聚乙烯外套船用电力电缆，DA型 EPR insulation tinned copper wire braided CSP outer sheath shipboard power cable, Type DA |  |
| CEH8H/DA | 乙丙绝缘氯磺化聚乙烯内护套镀锡铜丝编织铠装氯磺化聚乙烯外套船用电力电缆，DA型 EPR insulation CSP inner sheath tinned copper wire braided CSP outer sheath shipboard power cable, Type DA |  |
| CE82/DA | 乙丙绝缘镀锡铜丝编织铠装聚氯乙烯外护套船用电力电缆，DA型 EPR insulation tinned copper wire braided PVC outer sheath shipboard power cable, Type DA |  |
| CE8290/DA | 乙丙绝缘镀锡铜丝编织铠装聚氯乙烯内护套镀锌钢丝编织铠装船用电力电缆，DA型 EPR insulation tinned copper wire braided PVC inner sheath galvanized steel wire braided shipboard power cable, Type DA |  |
| CE8292/DA | 乙丙绝缘镀锡铜丝编织铠装聚氯乙烯内护套镀锌钢丝编织铠装聚氯乙烯外护套船用电力电缆，DA型 EPR insulation tinned copper wire braided PVC inner sheath galvanized steel wire braided PVC outer sheath shipboard power cable, Type DA |  |
| CEFR/DA | 乙丙绝缘氯丁护套船用电力软电缆，DA型 EPR insulation PCP sheath shipboard flexible power cable, Type DA |  |
| CEHR/DA | 乙丙绝缘氯磺化聚乙烯护套船用电力软电缆，DA型 EPR insulation CSP sheath shipboard flexible power cable, Type DA |  |
| CEVR/DA | 乙丙绝缘聚氯乙烯护套船用电力软电缆，DA型 EPR insulation PVC sheath shipboard flexible power cable, Type DA |  |
| CEFRP/DA | 乙丙绝缘镀锡铜丝编织独立屏蔽氯丁护套船用电力软电缆，DA型 EPR insulation tinned copper wire braided individual screen PCP sheath shipboard flexible power cable, Type DA |  |

| 型号 Type | 名称 Description | 产品标准 Standard |
| --- | --- | --- |
| CE8F/SA | 乙丙绝缘镀锡铜丝编织铠装氯丁外护套船用电力电缆，SA型 EPR insulation tinned copper wire braided PCP outer sheath shipboard power cable, Type SA | IEC60092-350 IEC60092-353 IEC600332-3A |
| CEF8F/SA | 乙丙绝缘氯丁内护套镀锡铜丝编织铠装氯丁外护套船用电力电缆，SA型 EPR insulation PCP inner sheath tinned copper wire braided PCP outer sheathed shipboard power cable, Type SA |  |
| CE8H/SA | 乙丙绝缘镀锡铜丝编织铠装氯磺化聚乙烯外套船用电力电缆，SA型 EPR insulation tinned copper wire braided CSP outer sheath shipboard power cable, Type SA |  |
| CEH8H/SA | 乙丙绝缘氯磺化聚乙烯内护套镀锡铜丝编织铠装氯磺化聚乙烯外套船用电力电缆，SA型 EPR insulation CSP inner sheath tinned copper wire braided CSP outer sheath shipboard power cable, Type SA |  |
| CE82/SA | 乙丙绝缘镀锡铜丝编织铠装聚氯乙烯外护套船用电力电缆，SA型 EPR insulation tinned copper wire braided PVC outer sheath shipboard power cable, Type SA |  |
| CE8290/SA | 乙丙绝缘镀锡铜丝编织铠装聚氯乙烯内护套镀锌钢丝编织铠装船用电力电缆，SA型 EPR insulation tinned copper wire braided PVC inner sheath galvanized steel wire braided shipboard power cable, Type SA |  |
| CE8292/SA | 乙丙绝缘镀锡铜丝编织铠装聚氯乙烯内护套镀锌钢丝编织铠装聚氯乙烯外护套船用电力电缆，SA型 EPR insulation tinned copper wire braided PVC inner sheath galvanized steel wire braided PVC outer sheath shipboard power cable, Type SA |  |
| CEFR/SA | 乙丙绝缘氯丁护套船用电力软电缆，SA型 EPR insulation PCP sheath shipboard flexible power cable, Type SA |  |
| CEHR/SA | 乙丙绝缘氯磺化聚乙烯护套船用电力软电缆，SA型 EPR insulation CSP sheath shipboard flexible power cable, Type SA |  |
| CEVR/SA | 乙丙绝缘聚氯乙烯护套船用电力软电缆，SA型 EPR insulation PVC sheath shipboard flexible power cable, Type SA |  |
| CEFRP/SA | 乙丙绝缘镀锡铜丝编织独立屏蔽氯丁护套船用电力软电缆，SA型 EPR insulation tinned copper wire braided individual screen PCP sheath shipboard flexible power cable, Type SA |  |

| 型号 Type | 名称 Description | 产品标准 Standard |
| --- | --- | --- |
| CEFP/DA | 乙丙绝缘镀锡铜丝编织独立屏蔽氯丁护套船用电力电缆，DA型 EPR insulation tinned copper wire braided individual screen PCP sheath shipboard power cable, Type DA | IEC60092-350 IEC60092-353 IEC60332-1 IEC60332-3A |
| CEFP80/DA | 乙丙绝缘镀锡铜丝编织独立屏蔽氯丁内护套镀锡铜丝编织铠装船用电力电缆，DA型 EPR insulation tinned copper wire braided individual screen PCP inner sheath tinned copper wire braided shipboard power cable, Type DA |  |
| CEFP90/DA | 乙丙绝缘镀锡铜丝编织独立屏蔽氯丁内护套镀锌钢丝编织铠装船用电力电缆，DA型 EPR insulation tinned copper wire braided individual screen PCP inner sheath galvanized steel wire braided shipboard power cable, Type DA |  |
| CEFP82/DA | 乙丙绝缘镀锡铜丝编织独立屏蔽氯丁内护套镀锡铜丝编织铠装聚氯乙烯外护套船用电力电缆，DA型 EPR insulation tinned copper wire braided individual screen PCP inner sheath tinned copper wire braided PVC outer sheath shipboard power cable, Type DA |  |
| CEFP92/DA | 乙丙绝缘镀锡铜丝编织独立屏蔽氯丁内护套镀锡铜丝编织铠装聚氯乙烯外护套船用电力电缆，DA型 EPR insulation tinned copper wire braided individual screen PCP inner sheath galvanized steel wire braided PVC outer sheath shipboard power cable, Type DA |  |
| CEFP/SA | 乙丙绝缘镀锡铜丝编织独立屏蔽氯丁护套船用电力电缆，SA型 EPR insulation tinned copper wire braided individual screen PCP sheath shipboard power cable, Type SA |  |
| CEFP80/SA | 乙丙绝缘镀锡铜丝编织独立屏蔽氯丁内护套镀锡铜丝编织铠装船用电力电缆，SA型 EPR insulation tinned copper wire braided individual screen PCP inner sheath tinned copper wire braided shipboard power cable, Type SA |  |
| CEFP90/SA | 乙丙绝缘镀锡铜丝编织独立屏蔽氯丁内护套镀锌钢丝编织铠装船用电力电缆，SA型 EPR insulation tinned copper wire braided individual screen PCP inner sheath galvanized steel wire braided shipboard power cable, Type SA |  |
| CEFP82/SA | 乙丙绝缘镀锡铜丝编织独立屏蔽氯丁内护套镀锡铜丝编织铠装聚氯乙烯外护套船用电力电缆，SA型 EPR insulation tinned copper wire braided individual screen PCP inner sheath tinned copper wire braided PVC outer sheath shipboard power cable, Type SA |  |
| CEFP92/SA | 乙丙绝缘镀锡铜丝编织独立屏蔽氯丁内护套镀锡铜丝编织铠装聚氯乙烯外护套船用电力电缆，SA型 EPR insulation tinned copper wire braided individual screen PCP inner sheath galvanized steel wire braided PVC outer sheath shipboard power cable, Type SA |  |

| 型号 Type | 名称 Description | 产品标准 Standard |
| --- | --- | --- |
| CEHP/DA | 乙丙绝缘镀锡铜丝编织独立屏蔽氯磺化聚乙烯护套船用电力电缆，DA型 EPR insulation tinned copper wire braided individual screen CSP sheath shipboard power cable, Type DA | IEC60092-350 IEC60092-353 IEC60332-1 IEC60332-3A |
| CEHP80/DA | 乙丙绝缘镀锡铜丝编织独立屏蔽氯磺化聚乙烯内护套镀锡铜丝编织铠装船用电力电缆，DA型 EPR insulation tinned copper wire braided individual screen CSP inner sheath tinned copper wire braided shipboard power cable, Type DA |  |
| CEHP90/DA | 乙丙绝缘镀锡铜丝编织独立屏蔽氯磺化聚乙烯内护套镀锌钢丝编织铠装船用电力电缆，DA型 EPR insulation tinned copper wire braided individual screen CSP inner sheath galvanized steel wire braided shipboard power cable, Type DA |  |
| CEHP82/DA | 乙丙绝缘镀锡铜丝编织独立屏蔽氯磺化聚乙烯内护套镀锡铜丝编织铠装聚氯乙烯外护套船用电力电缆，DA型 EPR insulation tinned copper wire braided individual screen CSP inner sheath tinned copper wire braided PVC outer sheath shipboard power cable, Type DA |  |
| CEHP92/DA | 乙丙绝缘镀锡铜丝编织独立屏蔽氯磺化聚乙烯内护套镀锡铜丝编织铠装聚氯乙烯外护套船用电力电缆，DA型 EPR insulation tinned copper wire braided individual screen CSP inner sheath galvanized steel wire braided PVC outer sheath shipboard power cable, Type DA |  |
| CEHP/SA | 乙丙绝缘镀锡铜丝编织独立屏蔽氯磺化聚乙烯护套船用电力电缆，SA型 EPR insulation tinned copper wire braided individual screen CSP sheath shipboard power cable, Type SA |  |
| CEHP80/SA | 乙丙绝缘镀锡铜丝编织独立屏蔽氯磺化聚乙烯内护套镀锡铜丝编织铠装船用电力电缆，SA型 EPR insulation tinned copper wire braided individual screen CSP inner sheath tinned copper wire braided shipboard power cable, Type SA |  |
| CEHP90/SA | 乙丙绝缘镀锡铜丝编织独立屏蔽氯磺化聚乙烯内护套镀锌钢丝编织铠装船用电力电缆，SA型 EPR insulation tinned copper wire braided individual screen CSP inner sheath galvanized steel wire braided shipboard power cable, Type SA |  |
| CEHP82/SA | 乙丙绝缘镀锡铜丝编织独立屏蔽氯磺化聚乙烯内护套镀锡铜丝编织铠装聚氯乙烯外护套船用电力电缆，SA型 EPR insulation tinned copper wire braided individual screen CSP inner sheath tinned copper wire braided PVC outer sheath shipboard power cable, Type SA |  |
| CEHP92/SA | 乙丙绝缘镀锡铜丝编织独立屏蔽氯磺化聚乙烯内护套镀锡铜丝编织铠装聚氯乙烯外护套船用电力电缆，SA型 EPR insulation tinned copper wire braided individual screen CSP inner sheath galvanized steel wire braided PVC outer sheath shipboard power cable, Type SA |  |

| 型号 Type | 名称 Description | 产品标准 Standard |
| --- | --- | --- |
| CEVP/DA | 乙丙绝缘镀锡铜丝编织独立屏蔽聚氯乙烯护套船用电力电缆，DA型 EPR insulation tinned copper wire braided individual screen PVC sheath shipboard power cable, Type DA | IEC60092-350 IEC60092-353 IEC60332-1 IEC60332-3A |
| CEVP80/DA | 乙丙绝缘镀锡铜丝编织独立屏蔽聚氯乙烯内护套镀锡铜丝编织铠装船用电力电缆，DA型 EPR insulation tinned copper wire braided individual screen PVC inner sheath tinned copper wire braided shipboard power cable, Type DA |  |
| CEVP90/DA | 乙丙绝缘镀锡铜丝编织独立屏蔽聚氯乙烯内护套镀锌钢丝编织铠装船用电力电缆，DA型 EPR insulation tinned copper wire braided individual screen PVC inner sheath galvanized steel wire braided shipboard power cable, Type DA |  |
| CEVP82/DA | 乙丙绝缘镀锡铜丝编织独立屏蔽聚氯乙烯内护套镀锡铜丝编织铠装聚氯乙烯外护套船用电力电缆，DA型 EPR insulation tinned copper wire braided individual screen PVC inner sheath tinned copper wire braided PVC outer sheath shipboard power cable, Type DA |  |
| CEVP92/DA | 乙丙绝缘镀锡铜丝编织独立屏蔽聚氯乙烯内护套镀锡铜丝编织铠装聚氯乙烯外护套船用电力电缆，DA型 EPR insulation tinned copper wire braided individual screen PVC inner sheath galvanized steel wire braided PVC outer sheath shipboard power cable, Type DA |  |
| CEVP/SA | 乙丙绝缘镀锡铜丝编织独立屏蔽聚氯乙烯护套船用电力电缆，SA型 EPR insulation tinned copper wire braided individual screen PVC sheath shipboard power cable, Type SA |  |
| CEVP80/SA | 乙丙绝缘镀锡铜丝编织独立屏蔽聚氯乙烯内护套镀锡铜丝编织铠装船用电力电缆，SA型 EPR insulation tinned copper wire braided individual screen PVC inner sheath tinned copper wire braided shipboard power cable, Type SA |  |
| CEVP90/SA | 乙丙绝缘镀锡铜丝编织独立屏蔽聚氯乙烯内护套镀锌钢丝编织铠装船用电力电缆，SA型 EPR insulation tinned copper wire braided individual screen PVC inner sheath galvanized steel wire braided shipboard power cable, Type SA |  |
| CEVP82/SA | 乙丙绝缘镀锡铜丝编织独立屏蔽聚氯乙烯内护套镀锡铜丝编织铠装聚氯乙烯外护套船用电力电缆，SA型 EPR insulation tinned copper wire braided individual screen PVC inner sheath tinned copper wire braided PVC outer sheath shipboard power cable, Type SA |  |
| CEVP92/SA | 乙丙绝缘镀锡铜丝编织独立屏蔽聚氯乙烯内护套镀锡铜丝编织铠装聚氯乙烯外护套船用电力电缆，SA型 EPR insulation tinned copper wire braided individual screen PVC inner sheath galvanized steel wire braided PVC outer sheath shipboard power cable, Type SA |  |